# Building inspection · 18 October 2026

# Project details

### Project

| Building | Lindenhof apartments · Example |
| --- | --- |
| Address | Musterstraße 12, 12345 Musterstadt |
| Example | Fictional project · 18 October 2026 |

### Participants

| Site manager | Lena Weber · Lindenbau · Beispiel lena.weber@lindenbau.example · +49 000 10001 |
| --- | --- |
| Planner | Mara König · Planwerk · Beispiel mara.koenig@planwerk.example · +49 000 10002 |
| Contractor | Jonas Berger · Fassadenwerk · Beispiel jonas.berger@fassadenwerk.example · +49 000 10003 |

# Documentation details

### Inspection

| Date | 18 Oct 2026 |
| --- | --- |
| Documentation number | LH-2026-001 |
| Purpose | Record visible building-envelope defects and define further investigation and follow-up. |
| Property | Lindenhof apartments - Musterstraße 12, 12345 Musterstadt |
| Inspection time | 09:15-11:15 |
| Inspection method | External visual inspection from accessible ground-level areas |
| Prepared by | Mara König - building surveyor |
| Follow-up reviewed | 19 October 2026 |

### Inspection participants

| Planner | Mara König · Planwerk · Beispiel mara.koenig@planwerk.example · +49 000 10002 |
| --- | --- |
| Site manager | Lena Weber · Lindenbau · Beispiel lena.weber@lindenbau.example · +49 000 10001 |

# Task overview

| Task | Location | Responsible | Status | Deadline | Page |
| --- | --- | --- | --- | --- | --- |
| Task 1 · Arrange assessment of the damaged balcony edge | Pin 1.1.1 · Defect | Lena Weber · Lindenbau · Beispiel | In progress | 23 Oct 2026 |  |
| Task 2 · Measure moisture and inspect the downpipe connection | Moisture | Mara König · Planwerk · Beispiel | Open · Overdue | 18 Oct 2026 |  |

## Pin 1

Figure 1    ● Concrete damage

## Pin 1.1

Figure 2

## Pin 1.1.1 · Defect

| Component | Concrete spalling · Balcony underside |
| --- | --- |

| Figure 3 · Concrete spalling · Balcony underside | Assessment and investigation - exposed reinforcement The visible condition is consistent with deterioration of the concrete cover associated with reinforcement corrosion. The initiating cause and the extent of corrosion cannot be established by visual inspection. Further loose or detached concrete may be present beyond the visible opening. A competent concrete specialist should inspect the underside and adjacent slab edges at close range, establish the extent of unsound concrete and assess cover and reinforcement condition. The slab top, waterproofing, edge details and drainage should also be checked for possible moisture entry. The specialist should determine any further testing and whether structural assessment is required. Maintain the precautionary restriction below the affected area until it has been assessed. Define repair measures from the investigation findings; this visual record does not establish that the balcony is safe for unrestricted use. |
| --- | --- |

### Tasks and measures

Task 1 · Arrange assessment of the damaged balcony edge

| Responsible | Lena Weber · Lindenbau · Beispiel |
| --- | --- |
| Status | In progress |
| Deadline | 23 Oct 2026 (Europe/Berlin) |
| Comments | Access is secured. Coordinate the inspection with the specialist before defining the repair. |
| Evidence | Figure 3 |

## Moisture

| Component | Moisture at the plinth |
| --- | --- |

| Figure 4 · West elevation - downpipe and plinth ● Moisture-related findings | Location and context - west plinth The marked area is at the foot of the rainwater downpipe on the west elevation, close to the north-west corner. The overview records the relationship between the staining, downpipe, gravel strip and adjacent ground. The linked detail photograph records the surface condition. |
| --- | --- |

| Figure 5 · Moisture at the plinth | Finding - staining and deposits at the plinth At the west elevation, beside the rainwater downpipe near the north-west corner, irregular dark staining is visible in the rendered plinth. The affected area is approximately 0.60 m wide and extends to about 0.45 m above the adjoining ground level, estimated visually. Patchy whitish deposits and local changes to the surface coating are visible. The boundary with the less affected render above is irregular. These features are compatible with repeated wetting and drying, but the deposits have not been identified by testing. No material moisture measurements or inspection of the concealed wall layers was undertaken. Inspect the downpipe joints and drainage connection, adjacent ground levels and plinth detailing, then record comparative moisture readings before deciding on remedial work. |
| --- | --- |

### Tasks and measures

Task 2 · Measure moisture and inspect the downpipe connection

| Responsible | Mara König · Planwerk · Beispiel |
| --- | --- |
| Status | Open · Overdue |
| Deadline | 18 Oct 2026 (Europe/Berlin) |
| Comments | Please add readings and a photo of the connection to this finding. |
| Evidence | Figure 5 |